## Appendix 7D-3	Standard VDOT Riprap Classifications,

## Weights, and Blanket Thickness

| Classification | D50 (ft) | W50 (lbs) | T (in) |
| --- | --- | --- | --- |
| #### Class AI | 0.8 | 50 | 20 |
| ##### Class I | 1.1 | 100 | 26 |
| Class II | 1.6 | 300 | 38 |
| Class III | 2.2 | 1000 | 53 |
| Type I | 2.8 | 2000 | 60 |
| Type II | 4.5 | 8000 | 97 |